description: reinforced, printed and lacquered membrane with increased protection against staining and abrasion of1.5 mm of thickness. microorganisms resistant. application of a protective acrylic lacquer on the top layer. maximum antislippery resistance. application: swimming pools applications. useful for outdoor applications according to the european standard EN 15836-2 – plastics-plasticized poly(vinyl chloride) (PVC-P) membranes for inground swimming pools – part 2: reinforced membranes of nominal thickness equal to or greater than 1.5 mm.

TABLE 1- CHARACTERISTICS OF THE MEMBRANE

| # CHARACTERISTIC | ### TEST METHOD | ##### VALUE |
| --- | --- | --- |
| # DENSITY | ###### EN 1849-2 | 1800 + 100 g/m2 |
| # WATER ABSORPTION | ###### EN ISO 62:08 | < 1% OF MASS |
| #### CaCO3 CONTENT | ATOMIC ABSORPTION | < 3% OF MASS |

TABLE 2- DIMENSIONAL CHARACTERISTICS

| # CHARACTERISTIC | ### TEST METHOD | ##### VALUE |
| --- | --- | --- |
| # MEAN THICKNESS (mm) | ###### EN 1849-2 | 1.5 (-5, +10%) |
| #### THICKNESS IN THE NET CROSS (mm) | EN 1849-2 | > 0.3 |
| #### WIDTH (mm) | EN 1849-2 | NOM + 5 mm |
| #### FLATNESS (mm) | EN 1849-2 | < 10 |
| #### LINEARITY (mm) | EN 1849-2 | < 30 |

TABLE 3- MECHANICAL CHARACTERISTICS

| # CHARACTERISTIC | ### TEST METHOD | ##### VALUE |
| --- | --- | --- |
| TENSILE STRENGHT (N/50 mm) | #### EN 12311-2 A | L,T > 1100 |
| ELONGATION AT BREAK (%) | #### EN 12311-2 A | L, T > 15 |
| JOINT STRENGHT, PEEL RESISTANCE (N/50 mm) | EN 12316-2 | ## L,T > 80 |
| TEAR RESISTANCE(N) | EN 12310-2 | L,T > 180 |
| DIMENSIONAL STABILITY (%) | EN 1107-2 | L, T < 0.5 |
| RESISTANCE TO FOLDABILITY (-25º C) | #### EN 495-5 | ###### WITHOUT CRACKS |
| PEEL RESISTANCE OF JOINTS(N/50 mm) | #### EN 12316-2 | ###### > 80 |
| SLIP RESISTANCE (RAMP TEST) | #### DIN 51097 | ###### GROUP C |

TABLE 4- CHARACTERISTICS FOR DURABILITY

| # CHARACTERISTIC | ### TEST METHOD | ##### VALUE |
| --- | --- | --- |
| RESISTANCE TO AN ARTIFICIAL AGEING OF 19 gj/m2 (6000 h) | EN ISO 4892-2:2006 MET. A CYCLE Nº 1 | > 3 ACCORDING EN 20105-A02 |
| RESISTANCE TO ACTION OF MICROORGANISMS | EN ISO 846:97 / D | ## MASS LOSS < 1% |
| RESISTANCE TO streptoverticilium reticulum bacteria | EN ISO 846:97 / C | ## WITHOUT STAINS |
| CHLORINE RESISTANCE | EN 15836 ANNEX C | ## RATING > 3 |
| RESISTANCE TO STAINING AGENTS | EN 15836 ANNEX D | ## RATING > 4 |